## Slide 1
  Absorption spectra of HiPco CNT
DNA-assisted dispersion and separation of carbon nanotubes, Ming Zheng
My Data
Purification and Characterization of Single-Wall Carbon Nanotubes (SWNTs) Obtained from the Gas-Phase Decomposition of CO (HiPco Process), R. H. Hauge
Wavelength (nm) | Diameter (nm)
1000 | 0.80
1200 | 0.96
1400 | 1.13
1600 | 1.29
Peak Wavelength(nm) | Diameter (nm)
1036 | 0.829
1128 | 0.904
1188 | 0.953
1272 | 1.02
1324 | 1.06
1036
1128
1188
1272
1324
The spectra reveals the presence of 5 different peak wavelength with a diameter distribution spanning from 0.829 to 1.06 nm.
v1->c1
metal
v2->c2 v1->c1
semiconduting
Last Update: 22 March 2023

## Slide 2
  Absorption spectra of HiPco CNT after DNA wrapping

## Slide 3
  Absorption spectra of CoMoCAT CNT
Highly selective dispersion of single-walled carbon nanotubes using aromatic polymers, Robin J. Nicholas
My Data
Wavelength (nm) | Diameter (nm)
1000 | 0.80
1200 | 0.96
1400 | 1.13
1600 | 1.29
Peak Wavelength (nm) | Diameter (nm)
984 | 0.787
1037 | 0.830
1137 | 0.912
1272 | 1.02
984
1037
1137
1272
The spectra reveals the presence of 4 different peak wavelength with a diameter distribution spanning from 0.787 to 1.02 nm.
Purification and Characterization of Single-Wall Carbon Nanotubes (SWNTs) Obtained from the Gas-Phase Decomposition of CO (HiPco Process), R. H. Hauge

## Slide 4
  Absorption spectra of CoMoCAT CNT after DNA wrapping

## Slide 5
  Absorption spectra of HiPco & CoMoCAT CNT
My Data (test solution - DI water or 1x Tris solution)

## Slide 6
  PLE mapping of HipCo CNT
(8,3)
(6,5)
(8,4)
(7,6)
(10,2)
(9,4)
(8,6)
(7,5)
(8,7)
(9,5)
(10,3)
  SC-SWCNT
  RNA-SWCNT
Excitation Wavelength (nm) | Emission Wavelength (nm) | Assignment
568 | 982 | (6,5)
668 | 961 | (8,3)
647 | 1032 | (7,5)
648 | 1131 | (7,6)
590 | 1122 | (8,4)
736 | 1065 | (10,2)
724 | 1114 | (9,4)
718 | 1183 | (8,6)
733 | 1274 | (8,7)
676 | 1253 | (9,5)
633 | 1258 | (10,3)
(8,3)
(6,5)
(8,4)
(7,6)
(10,2)
(9,4)
(8,6)
(7,5)
(9,5)
(10,3)
(8,7)
Excitation Wavelength (nm) | Emission Wavelength (nm) | Assignment
571 | 993 | (6,5)
671 | 971 | (8,3)
651 | 1044 | (7,5)
654 | 1139 | (7,6)
594 | 1131 | (8,4)
740 | 1077 | (10,2)
725 | 1127 | (9,4)
724 | 1197 | (8,6)
731 | 1284 | (8,7)
678 | 1265 | (9,5)
633 | 1268 | (10,3)

## Slide 7
  PLE mapping of HipCo CNT
Jaehoon’s DNA Wrapped sample
Jaehoon’s Unwrapped sample
My RNA Wrapped sample
My Unwrapped sample

## Slide 8
  PLE mapping of CoMoCAT CNT
  SC-SWCNT
  RNA-SWCNT
(6,5)
(8,4)
(7,6)
(7,5)
Excitation Wavelength (nm) | Emission Wavelength (nm) | Assignment
573 | 998 | (6,5)
652 | 1046 | (7,5)
594 | 1134 | (8,4)
654 | 1142 | (7,6)
728 | 1128 | (9,4)
(9,4)
(6,5)
(7,5)
(8,4)
(7,6)
(9,4)
Excitation Wavelength (nm) | Emission Wavelength (nm) | Assignment
570 | 983 | (6,5)
646 | 1031 | (7,5)
591 | 1123 | (8,4)
648 | 1130 | (7,6)
724 | 1113 | (9,4)
My data (My data – Table1)

## Slide 9
  PLE mapping of CoMoCAT CNT
Jaehoon’s Unwrapped sample
My Unwrapped sample
Jaehoon’s DNA Wrapped sample
My RNA Wrapped sample

## Slide 10
Wave number to wavelength
dt calculated using this formula:
Raman intensity peak correspond CNT assignment from Table 1
  Raman Spectra of HipCo CNT 785nm
My Data
The Raman spectra reveals the presence of 5 different semiconducting (n,m) with a diameter (dt) distribution spanning from 0.885 to 1.10 nm.
assignment | Predicted v_RBM (cm^-1) | v_RBM (cm^-1) | dt (nm)
(9,7) | 214.9 | 214.7 | 1.104249
(10,3) | 225.1 | 225.2 | 1.05127
(11,3) | 232.8 | 232.4 | 1.014526
(10,2) | 265.1 | 264.1 | 0.884798
(7,6) | 262.1 | 264.1 | 0.895433
(11,3)
(10,2)
(7,6)
(10,3)
(9,7)

## Slide 11
  Raman Spectra of CoMoCAT CNT 785nm
My Data
assignment | Predicted v_RBM (cm^-1) | v_RBM (cm^-1) | dt (nm)
(9,7) | 214.9 | 216.5 | 1.104249
(12,2) | 227 | 226.8 | 1.041958
(11,3) | 232.8 | 232.6 | 1.014526
(11,1) | 256.4 | 257 | 0.916359
(10,2) | 265.1 | 265.1 | 0.884798
The Raman spectra reveals the presence of 5 different semiconducting (n,m) with a diameter (dt) distribution spanning from 0.885 to 1.10 nm.
(9,7)
(12,2)
(11,3)
(11,1)
(10,2)

## Slide 12
Harshith’s SC CNT - CoMoCAT
SC CNT Synthesis Procedure:
Disperse 15 mg SWNT and 0.6 g Sodium Cholate (SC) in 30 mL H2O.
Probe-tip sonicate for 1 hour at 70% amplitude (Total power on tip sonicator = 130 W).
Transfer the surfactant into centrifuges according to same weight.
Ultracentrifuge for 2 hours at 30,000 RPM.
(9,1)
(6,4)
(8,3)
G peak
G’ peak
RBM

## Slide 13
RBM Peaks (cm-1) | Relatable Kataura Plot values | dt (nm) | Species assignment (n,m)
202.555 | 203.6 | 1.17 | (9,8)
212.486 | 212.1 | 1.12 | (13,2)
220.584 | 221.7 | 1.068 | (11,4)
Wavelength(nm) to Wave number (cm-1)
dt calculated using this formula:
SC CNT Characterisation in RBM Zone
(9,8)
(13,2)
(11,4)

## Slide 14
DNA wrapped CNT (Dialysis from SC-CNT)
(9,1)
(6,4)
(8,3)
G peak
G’ peak
RBM
(6,5)
Silicon
DNA
CNT Species
Water

## Slide 15
RBM Peaks (cm-1) | Relatable Kataura Plot values | dt (nm) | Species assignment (n,m)
208 | 207.7 | 1.145 | (12,4)
215 | 215.1 | 1.103 | (9,7)
223 | 221.7 | 1.068 | (11,4)
244 | 241.6 | 0.976 | (9,5)
253 | 251.3 | 0.936 | (10,3)
Wavelength(nm) to Wave number (cm-1)
dt calculated using this formula:
DNA wrapped CNT (Dialysis) – RBM Zone
Notes: 208 215 223 244 253

## Slide 16
SC CNT with 633 nm Laser
G’ peak
G peak
RBM

## Slide 17
632
Extinction coefficient for SC-CNT = 3.6 1e4 cm2/gm
At 632 nm Absorbance of sample is 0.48144
Concentration of SC-CNT in sample is 40.12 mg/L
Absorbance of SC-CNT (3X)

## Slide 18
Parameter trials for PL mapping
Excitation Slit Width (nm) | Emission Slit Width (nm) | Integration Time (sec) | Intensity
4 | 4 | 0.4 | 6000
3 | 3 | 0.5 | 3500
5 | 2 | 0.4 | 4000
5 | 2 | 0.5 | 4000
5 | 1 | 0.3 | 2500
5 | 1 | 0.4 | 2500
5 | 3 | 0.4 | 6000
Best Choice
Final decided parameters:
Excitation: 500-700 nm, Increment: 2 nm, Slit Width: 5 nm
Emission: 900-1200 nm, Increment: 2 nm, Slit Width: 3 nm
Integration time: 0.4 sec

## Slide 19
Jaehoon’s Data
PL Mapping of SC-CNT
CNT Species | Excitation (nm) | Emission (nm)
(6,5) | 570 | 985
(7,5) | 645 | 1035
(7,6) | 650 | 1130
(8,4) | 590 | 1125